Date 03.05.2018

Two Pack

Literature of 1001 Epoxy Finish Paint( Product Code – 0682G )

Epoxy Finish Paint system is supplied in Two separate containers, namely Base

& Hardener in the ratio of 3:1 by volume wait for 10 - 15 minutes as flash off time before applying the coating. If required, add spl. Epoxy Reducer 0682T in the mixed material up to 10% before use. Care is to be taken that the mixed material is to be consumed within 3-4 hours. Mixed material has got limited pot life of 4 hours. Application of Primer should be followed with a coat of Epoxy Finishing Paint (2 Pack).Dry Film Thickness (D.F.T) of 60 to 70 Microns should be achieved after Epoxy Primer followed by Epoxy Finishing. It is recommended that composite system of Epoxy Primer, Epoxy Finishing alongwith Epoxy Thinner / Reducer should be from the same source.

Few characteristic are cited below:-

1.   Consistency				:	Smooth and Uniform

2.   Viscosity at 30 C B/4 Cup. 		:	60 - 90 Seconds

3.   Covering Capacity as per IS: 101.	:	14-16Sq. Mts. Per liter (DFT 30 Microns)

Dry film Thickness.

- Drying Time of mixed material

( Base + Hardener )

a)  S.D.				:	2-4Hrs.

b) H.D.				:	6 – 8 Hrs.

c) T.F.				:	Overnight

5.   Finish				:	Full Gloss, Semi Gloss and Egg-Shell to Matt

6.   Weight per litre in Kg. 		:	0.93 to 1.2 + 0.5.(Depending on shade required)

7.    Method Of Application 		:	By spray, curtail or brush ( If there is appreciable

drags on brush, add more epoxy 	Reducer for

better application)

8.    Shelf life. 				:	Minimum one year after date of manufacture

(In separate sealed containers)

Uses : -

Recommended for use on steel structures, bridges, interior and exterior of storage tanks,

bulk handling equipment, pipelines etc. as well as other Installations exposed to saline & highly

corrosive environments.

For Glossy Color and Paints Pvt. Ltd.,