Date 03.05.2018

Two Pack

Literature of Infinity Epoxy Coating (Chemical Resisting Enamel ) 6075G

Scope (	Infinity Epoxy Coating is unaffected by a broad spectrum of corrosive chemical and solvent exposure. It is specifically meant for protection against fumes, dust, and corrosion etc.

It is recommended for application in refineries, petrochemicals and pharmaceutical environment.

Product Data

1.  Consistency 				:	60 – 70  Seconds With Ford Cup B4 at 27°C

2.  Drying Time	 A) S.D.            	      	:      	1 – 2 HR. | After Mixing Base & Hardener in

B) H.D.	  		2 – 4 HR.| the ratio 3:1 by Volume

C) Tack Free			0  /  N 16 – 24 Hours

3.  Finish  				:	Smooth And Glossy

4.  Gloss Reading at 45 % A/H		:	55 A / Head

5.  Shade				:	White

6.  Fineness Of Grind			:	10 Microns

7.  Non Volatile Matter 			:	60% + 3%

8.  Force Drying at 65ºC for 20 Minutes 	:	Can Be Force Dry at 65°C For 20 Minutes if fast

production is required although it is air drying

9.  Wt. Per10 Litre In Kg.		:	11.00 kg + 2%

10. Scratch Hardness 			:	Passes The Test

Cont/-…

- : 2 : -

11. Flexibility & Adhesion 		:	O.K.

(½ Mandrel)

12. Spreading Capacity As Per IS101	:	8 – 10 Sq. Mtr. Per. litre

(Chequer Board Method )				25 Microns DFT

13. Resistance To Water       		:	No Effect

14. Protection Against Corrosion           	: 	Passes The Test For More Than 7 Days

Under Condition Of Condensation

15. Resistance To Salt Spray              	:           	Passes The Test For More Than 5 Days

16. Shelf Life                                    	:           	One Year Under Properly Sealed Condition

17. Mixing Ratio 			:	Mix Base & Hardener in the ratio 3:1 by

volume, wait for 30 minutes minimum before

spraying. Ensure that the primed surface must

be nail proof hard 20 – 25 % Epoxy Reducer

0682T is to be added before spraying

For Glossy Color & Paints Pvt. Ltd.,