Glossy Anticorrosion Epoxy Primer 2K

Product description

Glossy Anticorrosion Epoxy Primer  2K  with excellent anticorrosion properties, outstanding

chemical resistance and good adhesion over steel, stainless steel, galvanized steel and suitable

substrates.

To reach optimum performance of Glossy paint systems, surface should be thoroughly cleaned

and degreased.

Surface to be painted is best prepared by blast cleaning for maximum durability and optimum

paint usage. Alternatively, mechanical sanding with P180 D/A or manually with Scotch-Brite.

Can also be carried out before and after sanding the surface must be degreased with Glossy

degreaser 3 in one. Galvanized steel should be previously degreased with Glossy 3 in one

degreaser and then sanded with P320 Empery Paper

Aluminium Surface should be etched primed or flatted before epoxy primer follows

Product ( 	(1) Glossy 2k Epoxy Base	(2) Glossy Epoxy Hardener   (3) Glossy 0682T Thinner

Method of application ( Mix epoxy primer Base & Hardener in the ratio of 3 : 1 by volume,

wait for 20 minutes as maturing time. Adjust spraying viscosity between 17 – 20  seconds with

cup B4 at 27ºC

Pot life at 27ºC ( 4 to 6 hours

Apply 2 coats to give dry film thickness of 50 -70 microns d.f.t.

Flash off time 10 -15  minutes between coats for 20 -30 minutes before baking

Air dry at 20ºC

Dust Free : 45 minutes – 1 hours

Tack free  :  3 – 4 hours

Hard dry   :  16 – 24 hours

Force dry at 60ºC

Hard dry : 30 minutes

Machine sanding ( after Hard dry ) Emery Paper 240 / finer must be carried out before recoating

Recoat Time

Can be recoated after 3 – 24 hours at 20º C. but sanding must be done before recoating for best

appearance, allow to fully dry before recoating. Drying time will depend on film thickness and

drying conditions. The longer drying  time, the better final appearance.

Good ventilation must be provided in the working environment.

Glossy Color and Paints Pvt. Ltd.,

Authorised Signatory.

-----------------------------------------------------------------------------------------------------------------

"High Quality Anticorrosive Black Matt

Finish  H.R. UP TO 800ºC "

It is better known as Black Anticorrosive Coating with maximum thermal

stability. It is manufactured with high quality inorganic anticorrosive pigment black

and inert extenders with silicone as main vehicles. It is an unique industrial and

maintenance heat resistance single coat matt finish paint.

Thinning 		: 	Glossy Thinner 014HST

Uses			:	Where High Heat resisting coating is required

Finish 			:	Smooth and one coat matt finish

Application 		: 	By brush or Spray

Covering Capicity 	:	18 – 20 sq. mtr. Per liter with 25 – 30 microns d.f.t.

Drying time 		:	Touch Dry – 1 Hr. Hard Dry – 4-6 Hrs. Tack Free – Over Night

Color Range 		:	Matt Black

Packing 		:	1 litre, 4 litre only

Shelf life 		:	Six Months in Original sealed container

Undercoats		:	Self

Main fields of application are machine-components, engine manifolds,

car, exhaust Silencer smokestacks, electrical equipments & dry units etc.

Glossy Color and Paints Pvt. Ltd.,

Authorised Signatory.

-------------------------------------------------------------------------------------------

Literature of Paint Remover

Paint Remover is better known as industrial grade paint stripper. It is

based on wax with combinations of vaporizing aromatic additives & solvents.

It is having excellent stripping ( Removing Paint ) power & degreasing of metallic

surface etc. Some of its salient features are cited below :-

- Form of Supply  (  Homogeneous

- It is slightly acidic in nature so precaution is to be taken to avoid skin & Eyes contact

- Apply liberally on the painted surface and leave it contact at least for 10 – 20 minutes

- Do not apply on wet surface

- Now try to remove the stripped paint either with some putty scrapper or with rough cloths Hose out the entire stripped surface with jet of water so that no residual is left over

- It has no ill effect on rubber chromium or on Zinc substrates

- Keep the bottle or jerkin away from heat & fire

- Keep the container closed after use

- Pack : 1 litre , 5 litre & 20 litre Plastic Containers

Note :- Shake well before every application

Glossy Color and Paints Pvt. Ltd.

Authorised Signatory